管道符号 Piping Symbols

| 法兰 Flanged 螺纹 Threaded 锥形和 喇叭口 Bell & Spigot 熔焊 Welded 焊接 Soldered 1. 角阀 Angle Valve 1.1 止回阀 1.1 Check 1.4 截止阀 (正视图) 1.4 Globe (elevation) 1.5 截止阀 (平面图) 1.5 Globe (plan) 1.6 软管角阀 1.6 Hose Angle 与符号9.1相同 Same as Symbol 9.1 2. 自动阀 Automatic Valve 2.1 旁路 2.1 By-Pass 2.2 控制器操作 2.2 Governor-Operated 2.3 减压 2.3 Reducing 3. 止回阀 Check Valve 3.1 角形止回阀 3.1 Angle Check 与符号1.1相同 Same as symbol 1.1 3.2 (直线管路) 3.2 (straight way) 4. 旋塞阀 Cock 5. 隔膜阀 Diaphragm Valve 6. 浮球阀 Float Valve 7. 闸阀 Gate Valve 7*.1 7.4 电机操作 7.4 Motor-Operated * 如果有进一步的说明，也可用作通用的停止阀。 *Also used for general STOP VALVE symbol when amplified by specification. |  | 法兰 Flanged 螺纹 Threaded 锥形和 喇叭口 Bell & Spigot 熔焊 Welded 焊接 Soldered 8. 截止阀 Globe Valve 8.1 8.2 角形截止阀 8.2 Angle Globe 符号与1.4和1.5相同 Same as Symbols 1.4 & 1.5 8.3 软管截止阀 8.3 Hose Globe 符号与9.3相同 Same as Symbol 9.3 8.4 电机操作 8.4 Motor-Operated 9. 软管阀门 Hose Valve 9.1 角阀 9.1 Angle 9.2 闸阀 9.2 Gate 9.3 截止阀 9.3 Globe 10. 双重阀 Lockshield Valve 11. 快开阀 Quick-Opening Valve 12. 安全阀 Safety Valve 13. 停止阀 Stop Valve 符号与7.1相同 Same as Symbol 7.1 14. T形 Tee 14.7 侧向出口(出口朝下) 14.7 Side Outlet (outlet down) 14.8 侧向出口(出口朝上) 14.8 Side Outlet (outlet up) 15. 一体式 Union |
| --- | --- | --- |

阀门的识别涂漆

1、阀门产品按阀体材料进行识别涂漆，其颜色按下表

| 阀体材料 | 灰铸铁、可锻铸铁 | 球墨铸铁 | 碳素钢 | 耐酸钢、不锈钢 | 合金钢 |
| --- | --- | --- | --- | --- | --- |
| 识别涂漆颜色 | 黑色 | 银色 | 中灰色 | 天蓝色 | 中蓝色 |

注：耐酸钢、不锈钢允许不涂漆，铜合金不涂漆

    2、为了表示阀门产品密封面的材料，应在传动的手轮、手柄、板手上进行识别涂漆、其颜色按下表的规定。

| 密封面材料 | 铜合金 | 巴氏合金 | 耐酸钢不锈钢 | 渗氮钢渗硼钢 | 硬质合金 | 蒙耐尔合金 | 塑料 | 橡胶 | 铸铁 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 识别涂漆颜色 | 大红色 | 淡黄色 | 天蓝色 | 天蓝色 | 天蓝色 | 深黄色 | 紫红色 | 中绿色 | 黑色 |

注：（1）阀座和启闭件密封面材料不同时，按低硬度材料涂色。
        （2）止回阀、涂在阀盖顶部：安全阀、减压阀、疏水阀涂在阀罩或阀帽上。

    3、传动机构的涂漆颜色，按下列规定：
      （1）电动装置：普通型涂中灰色，三合一（户外、防爆、防腐）型涂末蓝色。
      （2）气动、液动、齿轮传动等其它传动机构，同产品涂色。